## Slide 1
第一性原理计算模拟的发展和应用
张萃
松山湖材料实验室，东莞
2019 年 7 月 23 日

## Slide 2
Introduction of First-principles Calculations
01
Density Functional Theory Framework
02
First-principles Molecular Dynamics
03
Examples
04
— Outline —

## Slide 3
First-principles Simulations
Simulations of Real Materials Based on Quantum Mechanics
Erwin Schrödinger
Max Born
Julius R. Oppenheimer
Supercomputers
Increased Complexity of Material System

## Slide 4
First-principles Simulations
Simulations of Real Materials Based on Quantum Mechanics
Electronic Structure
Simulation of Atomic Nuclei in Materials Based on Electronic Structure
Density Functional Theory
Wave Function Method
Quantum Monte Carlo
Molecular Dynamics
Structure Prediction
Quantum-Classical Hybridization Method
1998 Nobel Prize in Chemistry
Walter Kohn (DFT)
John A. Pople (Quantum chemistry methods)
2013 Nobel Prize in Chemistry
Martin Karplus
Michael Levitt
Arieh Warshel
Multiscale models for complex chemical systems

## Slide 5
First-principles Simulations
Simulations of Real Materials Based on Quantum Mechanics
Application
SC, PEC
Simulation
surface, low-dimension…
Method Development
strong correlation, electron-phone coupling…
Simulation
Experiment
Theory
Basis
Feasibility
Foundation
Law
Data
Theory Test
Explanation
Prediction
Phenomena
Model
Phenomena
Model

## Slide 6
How to make impact?
Materials
Problem
Dissemination:
Publication,
Code development etc
Methods:
DFT, potentials,
MD, MC,
Coarse-graining etc
Education: Computational
Materials science
Chemistry etc
Knowledge: What to compute?
Basic properties of matter
Reaction mechanisms
Functional processes etc
Tools
People

## Slide 7
Theory of Properties
Multi-scale Material View
Electrons
Atoms
Microstructure
Continuum
Properties

## Slide 8
Theory of Properties
Electrons
Atoms
Microstructure
Continuum
Properties
Calculated
quantities
(ab initio)
Learning Methods
Neural network
Correlation method
…
Macroscopic
output
Multi-scale Material View

## Slide 9
Theory of Properties
Three Main Goals
Ensemble average (thermodynamics)
Real-time evolution (dynamics)
Ground/excited states of complex structure
  Structure: liquids, glasses, solids, defects, surfaces, interfaces
  Bond-breaking, charge transfer

## Slide 10
Energy Models
Energy models are important because it is representation of the structure, material properties and chemical process.
Empirical Models: functional forms with parameters fitted to experimental data (or calculated data)
    Pair potentials
    Many-body potentials
    Effective medium theories
Semi-Empirical Models:
    Tight binding
    MINDO
Quantum mechanical: start from Schrodinger equation and make approximations
    Hartree Fork Approximations
    Density Functional Theory
    Quantum Monte Carlo
Increased Speed
Increased transferability
Energy only E
Energy and electronic structure
Which one is the best?
Notes: Modified Intermediate Neglect of Differential Overlap，

## Slide 11
Introduction of First-principles Calculations
01
Density Functional Theory Framework
02
First-principles Molecular Dynamics
03
Examples
04
— Outline —

## Slide 12
Schrödinger Equation:
Microscopic Description of Atoms
Physical Model:
Electrons + Nucleus
Math Description:
Kinetic energy
Coulomb interaction
Coulomb interaction
Kinetic energy
Electron
Nucleus
Electron-nucleus coupling

## Slide 13
“Adiabatic approximation”
Born-Oppenheimer approximation
Separate electronic and nuclear motions
Only include electrons as quantum particles
❌
❌
el
Many-body problem
A function of nuclear geometry
Electronic Structure

## Slide 14
Hartree-Fork Approximations
Slater Determinant of many-particle wave function:
Limitation: lacking electron correlation
Post HF methods: more elaborate approximation for many-body wave function
Configuration Interaction (CI) method
Moller-Plesset (MP) perturbation theory
Couple-Cluster(CC) method
Can be very accurate, But, …scaling

## Slide 15
Hartree-Fork Approximations: Scaling
Method | Today (electrons) | 30 years
HF + CI (N6) | 10 | 100
Potentials | 108 | 1014
DFT (N3) | 1000 | 100,000
Doubling every 18 months
30 years
106 increase in performance
What does more computing buy us ?
Atoms
Small molecules
Molecules
Condensed matter

## Slide 16
Density Functional Theory: HK Theorems
Hohenberg-Kohn Theorem I:
Hohenberg-Kohn Theorem II:
Exact theory of many-body systems
External potential Vext (r) is determined uniquely by the ground state particle density n0(r).
For any given Vext (r), the exact ground state energy is the global minimum of E[n(r)], and the density n(r) minimizing E[n(r)] is the exact ground state density n0(r).
Vext (r)
n0(r)
n0(r)
HK

## Slide 17
Density Functional Theory: KS Scheme
Kohn-Sham scheme: A practical scheme
Kinetic energy
Non-interacting system
Exchange-correlation
term
KS scheme maps the complex, interacting electronic systems into a non-interacting systems, moving in an effective local potential.
Hartree energy
Unknown universal functional
(HK Theorem I)

## Slide 18
Density Functional Theory: KS Scheme
Kohn-Sham Hamiltonian of independent-particle system:
Kohn-Sham Equation:
Two assumptions: “System of non-interacting particles” and “”
Veff (r)
n0(r)
n0(r)
HK
Vext (r)
n0(r)
n0(r)
HK
KS

## Slide 19
Flowchart of Solving KS Equation
Initial guess
Calculate effective potential
Solve KS equation
Calculate electronic density
Self-consistent?
Output: energy, forces, eigenvalues…
Yes
No

## Slide 20
Exchange and Correlation Functional
In KS scheme, all the many-body interaction complexity is put into exchange-correlation energy .
Exact expression is unknown, approximation is required!
Local density approximation (LDA)
Generalized gradient approximation (GGA)
Meta-GGA
Homogeneous electron gas
Gradient of the density
Kinetic energy density and/or the Laplacians of the density
(PBE, PW, BLYP….)
(SCAN）

## Slide 21
Exchange and Correlation Functional
DFT-D
Hybrid density functional
+
Three-parameter hybrid functional (B3LYP)
Screened hybrid functional (HSE)
(PBE0)
Exact exchange
(TS, DFT-D2)
vdW density functional
Dispersion corrections
(vdW-DF2, optPBE-vdW, optB88-vdW)

## Slide 22
LDA
GGA
mGGA
Hybrid
Local density
Density gradient
Inexplicit occupied orbital info
Explicit occupied orbital info
?
Unoccupied orbital info
Hartree Theory
Chemical Accuracy
Jacob’s Ladder

## Slide 23
Relative free energies of H-bonded and non-H-bonded configurations samples during diffusion are not very accurate: different errors for most functionals.
Formidable task to describe, at the same level of accuracy, many different types of interactions: covalent bonding, hydrogen bonding, vdW interactions.
Water Dimer Interactions

## Slide 24
Pseudopotentials
Core electrons can be replaced by an angular dependent pseudopotentials.
Core electrons + Valence electrons
Si: 1s2 2s2 2p6 3s2 3p2
valence electron # = 4
Ti: 1s2 2s2 2p6 3s2 3p6 3d2 4s2
valence electron # = 10
Rc

## Slide 25
Pseudopotentials
“Norm-conserving (NC)”:
High accuracy, high transferability
Large cut-off radius of PW basis set
“Ultra-soft (US)”: Smooth wave function in the core region, but not accurate in there
“Projector augmented wave (PAW) method”: All-electron + pseudopotential methods
Integral of core region charge density = All-electron one
Small cut-off radius of PW basis set
All-electron spherical augmentation function
Augmentation sphere + Interstitial region
Pseudo wave function

## Slide 26
Basis Sets
Localized orbitals:
Scaling “ order- N ”
Linear combination of atomic orbitals (LCAO)
Size: number of orbitals per atom
single- to multiple- with polarization and diffuse orbitals
Plane waves:
Bloch Theorem:
T lattice vector
G reciprocal lattice vector
=
Periodic potential ,
Cut-off radius

## Slide 27
Introduction of First-principles Calculations
01
Density Functional Theory Framework
02
First-principles Molecular Dynamics
03
Examples
04
— Outline —

## Slide 28
First-principles Molecular Dynamics
Within the density functional theory (DFT) framework, forces in FPMD are derived from Kohn-Sham Energy:
Time
Energy
Born-Oppenheimer MD
Newton’s equation:
“Ab initio”

## Slide 29
Algorithm
The Verlet Algorithm:
The Velocity Verlet Algorithm:
The Leap Frog Algorithm:
velocities updated at half time step

## Slide 30
Ensembles
Canonical ensemble (NVT): closed system in contact with heat bath
Ergodic hypothesis:
Bath EB
System Ec
NVT
NVE
Micro-canonical ensemble (NVE): isolated closed system
at thermodynamic equilibrium
Nose-Hoover chain
Andersen thermostat
Langevin thermostat
…

## Slide 31
Periodic Boundary Conditions (PBCs)
Condensed matter (1023 particles)
MD supercell (100 ~106 particles)
MD supercell + PBCs macroscopic system
Short range potential cutoff: rcut < L/2
Long rang potential: Ewald summation
Reaction field method
Suitable for thermodynamic and structural properties, dynamic process
Not suitable for phase transition discussion
Minimum Image Convention

## Slide 32
First-principles Molecular Dynamics
Limitation
Time scales
Length scale (PBCs help)
Accuracy
Classical nuclei
Jacobi’s ladder
Path-integral MD

## Slide 33
Introduction of First-principles Calculations
01
Density Functional Theory Framework
02
First-principles Molecular Dynamics
03
Examples
04
— Outline —

## Slide 34
Multi-level simulations of water structure, IR spectra and entropy
Exp vs. vdW
Exp vs. GGA / hybrid
Exp vs. GGA / hybrid
Exp vs. vdW
1. Liquid Structure from First Principles

## Slide 35
H2O/VBM
Vacuum level
CBM
VBM
Reduction potential
Oxidation potential
Multi-level simulations on the band edge alignment:
2. Aqueous Environments from First Principles

## Slide 36
Bulk water ρ=0.99 g/cm3
Bulk water ρ=0.90 g/cm3
NVT ensemble
Particle Mesh Ewald
20-80 ns
GROMACS 4.5
SPC/E potential
N = 3456 - 221184
L. Fumagalli et al. Science 360, 1339 (2018)
3. Water Under Confinement

## Slide 37
Cluster formation
Electronic structure
Dynamics
Moisture-enhanced corrosion
Thermodynamics
First principles calculations
Pu2O3
PuO2
Pu
4. Actinide Surface Corrosion

## Slide 38
Science, 2017, 355(6326): 715-718.
Layer A
Layer B
Layer G
5. High Pressure Solid Hydrogen
Notes: Hexagonal close-packed

## Slide 39
Conclusion
Computational modeling is very powerful, but
Be Smart !

## Slide 40
QUANTUM ESPRESSO (http://www.pwscf.org) (free) (DFT, planewave, ultrasoft, norm-conserving)
SIESTA (https://departments.icmab.es/leem/siesta/) ) (free) (DFT, localized basis set, norm-conserving)
ABINIT (http://www.abinit.org) (free) (DFT, planewave)
CPMD (http://www.cpmd.org) (free) (DFT, planewave, time-dependent DFT)
VASP (http://cms.mpi.univie.ac.at/vasp) ($) (DFT, planewave, ultrasoft, PAW)
Materials Studio/Cerius (http://www.accelrys.com) ($) (DFT, planewave, ultrasoft)
Crystal (http://www.chimifm.unito.it/teorica/crystal) ($) (Hartree-Fock)
Gaussian (http://www.gaussian.com) ($) (chemistry, Hartree-Fock, DFT, correlated approaches)
Gamess-UK (http://www.cse.clrc.ac.uk/qcg/gamess-uk/) ($) (chemistry, Hartree-Fock, DFT, correlated approaches)
Software

## Slide 41
Bibliography
Allen and Tildesley, “Computer Simulations of Liquid” (Oxford)
Frenkel and Smit, “Understanding Molecular Simulations” (Academic)
R. M. Martin, “Electronic Structure - Basics Theory and Practical Methods”
W. Koch, M. C. Holthausen, “A Chemist’s Guide to Density Functional Theory”
P. G. Parr, W. Yang, “Density Functional Theory of Atoms and Molecules”
K. Burke, “The ABC of DFT”
F. Jensen, “Introduction to Computational Chemistry”
J. M. Thijssen, “Computational Physics”
D. Chandler, “Introduction to Modern Statistical Mechanics”
D. A. McQuarrie, “Statistical Thermodynamics” OR “Statistical Mechanics”
M. E. J. Newman and G.T. Barkema, “Monte Carlo Methods in Statistical Physics”
K. Binder and D.W. Heerman, “Monte Carlo Simulation in Statistical Physics”